## Slide 1: Correlated quantum phenomena in the strong spin-orbit regime
Tejas Deshpande
(24 September 2013)

## Slide 2
Outline
Introduction
Weak to intermediate correlations
  Pyrochlore iridates
    Experimental resume
    Electronic structure
    Magnetism and Weyl fermions
    The role of many-body effects
    Interactions with rare earth moments
    Issues and Outlook
Strong Mott Regime
  Full degeneracy lifting and honeycomb iridates
  Partial degeneracy lifting and ordered double perovskites
    Double perovskites
    Multipolar exchange
    Mean field theory
    Beyond mean-field theory
    Connections to experiments
Concluding Remarks and Outlook

## Slide 3
I. Introduction
Two central threads of quantum materials research
  Correlated electron physics (e.g. mainly 3d transition metal oxides)
    Local moment formation and magnetism
    Quantum criticality
    Unconventional superconductivity
  Non-trivial physics from strong Spin-Orbit Coupling (SOC)
    f-electron materials
    Topological insulators and superconductors (s- and p- orbitals)
What about systems with correlation + SOC?
  Heavy Transition Metal Oxides (TMOs) mainly from 5d series
  Both SOC and electronic repulsion strengths, λ and U respectively, become comparable
  Several arguments suggest that λ and U tend to cooperate rather than compete
A mean-field model: Hubbard model with SOC
No correlations and no SOC
with SOC
with correlations

## Slide 4
I. Introduction
No correlations and no SOC
with SOC
with correlations
A mean-field model: Hubbard model with SOC
1930s
1980s
2000s
2010s??
weak-to-intermediate correlation regime
strong Mott limit

## Slide 5
Angular momentum (Li) and spin (Si) of electrons on site i couple
Energy cost of repulsion between electrons on the same site = U
  One electron localized per site
I. Introduction
A mean-field model: Hubbard model with SOC
No correlations and no SOC
with SOC
with correlations
Consider example: Sr2IrO4
Kinetic energy with which electron hops from site j to i
The operator counts the number of electrons on site i in orbital α
Last terms kicks in when

## Slide 6
I. Introduction
Proposals for Iridates
Phase | Correlation | Properties | Proposed Materials
Axion Insulator | W-I | Magnetic insulator, TME, no protected surface states | R2Ir2O7
Weyl semi-metal | I | Dirac-like bulk states, surface Fermi arcs, anomalous Hall | R2Ir2O7
Chern Insulator | W-I | Bulk gap, QHE | SrIrO3
Fractional Chern Insulator | I-S | Bulk gap, FQHE | SrIrO3
Fractional Topological Insulator, Topological Mott Insulator | I-S | Several possible phases. Charge gap, fractional excitations | R2Ir2O7
Quantum spin liquid | S | Several possible phases. Charge gap, fractional excitations | Na2IrO3
Emergent quantum phases in correlated spin-orbit coupled materials. Abbreviations are as follows: TME = topological magnetoelectric effect, (F)QHE = (fractional) quantum Hall effect. Correlations are W-I = weak-intermediate, I = intermediate (requiring magnetic order, say, but mean field-like), and S = strong.

## Slide 7
II. Weak to Intermediate Correlations
Topological insulators: non-trivial topology of the bands in a gapped system
Gapless systems: Weyl semi-metals (WSMs)
Notion of band topology  some degree of itinerancy
Non-TI, but still topological phases, require: intrinsic symmetry breaking
Any form of intrinsic magnetization  correlations “weak” enough for mean-field
Examples of non-TI topological phases:
  Antiferromagnetic Topological Insulator (AFTI)
  Axion Insulator
  Weyl semi-metal
Strong Mott regime  electrons atomically localized; “band” topology doesn’t make sense
Exotic phases due to orbital- and spin-ordering when both are entangled
The spin + orbit entanglement lifts degeneracies of the ground states to give interesting lattice models

## Slide 8
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Formula: R2Ir2O7 where R is a rare earth element

## Slide 9
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Experimental resume
1.
Resistivity goes from being “metallic” (dρ/dT > 0) at T > Tc to “non-metallic” (dρ/dT < 0) at T < Tc
The rare earth ion affects crystal field splitting; Tc is changed
Larger R3+ cation  more metallicity; larger cation  decreased trigonal compression  increased the Ir-O orbital-overlap

## Slide 10
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Electronic structure
2.
Focus on Ir-electron physics; neglect the rare earth magnetism (relevant at very low temperatures)
Outer-shell electrons of Ir4+ cation are in a 5d5 configuration
SOC splits the t2g spinful manifold into a higher energy Jeff = 1/2 doublet and a lower Jeff = 3/2 quadruplet
Only (half-filled) Jeff = 1/2 doublet near the Fermi energy; 2 bands per Ir atom
4 Ir atoms in the tetrahedral unit cell  total 8 Bloch bands near Fermi energy
Full angular momentum operator projected to the t2g manifold:

## Slide 11
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Electronic structure
2.
Consider band structure of the 8 Bloch bands near the Γ point
Classification of 8 Bloch bands: two 2-D irreps and one 4-D irrep (cubic symmetry)
Pesin and Balents obtained “4-2-2”
The “2-2-4” and “4-2-2” can be TIs due to insulating ground state
Yang et al. found “2-4-2” metallic state due to trigonal distortion
Wan et al. also found “2-4-2” metallic state from LDA calculations
TI state in (metallic) Y2Ir2O7 is impossible
Increase distortion 
2+2
2
2

## Slide 12
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Electronic structure
2.
Convenient tight-binding model for both metallic and insulating regimes
Diagonalization gives “2-4-2” semi-metallic state for –2 ≤ t2/t1 ≤ 0 and a Topological Insulator otherwise
Semi-metallic state is a zero-gap semiconductor
This semi-metallic state forms stable non-Fermi liquid phase with a quadratic band touching at the Γ point: “Luttinger-Abrikosov-Beneslavskii” (LAB) phase
About LAB:
  Electron-hole pair excitations susceptible to “excitonic instability” due to unscreened Coulomb interactions
  Excitonic instability circumvented in the presence of time-reversal and cubic symmetries
  Enormous zero field anomalous Hall effect
Gives non-trivial Berry phase

## Slide 13
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Electronic structure
2.
Convenient tight-binding model for both metallic and insulating regimes

## Slide 14
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Magnetism and Weyl Fermions
3.
Local C3 axes for four Ir ions constituting a tetrahedron
Experiments suggest “all-in/all-out” (AIAO) ground state
Wan et al. found Weyl semi-metal with 24 Weyl nodes and suggested an axion insulator state
The role of many-body effects
4.
TI, AIAO, WSM stable to (perturbative) interactions
Axion insulator state appears in the CDMFT analysis but not at the Hartree-Fock level
Wang et al. formulated Z2 invariant in terms of zero-frequency Green’s function
Both CDMFT and Hartree-Fock theory cannot capture topological Mott insulator

## Slide 15
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Interactions with rare earth moments
5.
What about interactions between R-site f-electrons and the Ir d-electrons?
Non-Kramers R3+ ions (R = Pr, Tb, Ho) have an even and Kramers ions (R = Nd, Sm, Gd, Dy, Yb) have an odd number of f-electrons
Example: Yb2Ir2O7; two ordering temperatures: TM = 130 K (Ir sublattice) and T* ≈ 20 K (Yb sublattice)
Most studied f-electron physics in iridates: Pr2IrO7 (no MIT)
Zero field anomalous Hall effect at 0.3 K < T < 1.5 K
Pr moments exhibit spin-ice type physics; “2-in/2-out” configurations on each tetrahedron
Pr ordering via RKKY interaction
Chen et al. suggest coupling to Ir may help to stabilize the WSM and axion insulator phases

## Slide 16
II. Weak to Intermediate Correlations
Pyrochlore iridates
A.
Issues and Outlook
6.
Pyrochlore iridates undergo MIT with the onset of AIAO magnetic order
Nd2Ir2O7: AIAO at the Nd-sites may imply AIAO at the Ir-sites
Resonant x-ray diffraction measurements suggest Eu2Ir2O7 has AIAO order
  Generation of the spin-orbit exciton

## Slide 17
III. Strong Mott Regime
Electrons effectively localized to single atoms
Description in terms of local spin and orbital degrees of freedom (DOF) applies
Charge gap ≫ energy of spin and orbital excitations
Notion of band topology does not make sense
Orbital degeneracy resolved in a unique way
3-fold degenerate for 1, 2, 4, and 5 electrons
2-fold degenerate for 1 and 3 electrons
Orbital DOF behaves as additional “pseudo-spin” quantum variable
Exchange of spin + pseudo-spin  Kugel-Khomskii models
Jahn-Teller effect  lattice distortions split orbital degeneracy
“Quantumness” washed away by phonon modes
SOC trades Jahn-Teller effect for entanglement of spin and orbital DOF
Exchange of spin + pseudo-spin  possibilities of exotic new ground states
Quantum spin liquid and multipolar ordered phases possible in honeycomb iridates and the double perovskites

## Slide 18
III. Strong Mott Regime
Full degeneracy lifting and honeycomb iridates
A.
Ir4+ with 5d5  orbital degeneracy removed completely
Na2IrO3 and Li2IrO3  Ir4+ + strong Mott regime
Anisotropic exchange model
The only example of an exactly soluble model for a quantum spin liquid state!
No magnetic order + charge-neutral “spin”-carrying elementary excitations  Majorana fermions!
Unfortunately experiments on Na2IrO3 have not confirmed the Kitaev model yet

## Slide 19
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.
Need only 1 or 2 electrons in the 4d or 5d shells  strongly spin-orbit coupled analogs of Ti3+ and V3+ or V4+
V3+ or V4+ constitute classic families undergoing Mott transitions
With SOC, degeneracy lifting same as before
d1 case  local Jeff = 3/2 spin
d2 case  two parallel (spin-1/2) electrons with aligned spins due to Hund’s rule  total spin S = 1
Since t2g has Leff = 1, Jeff = Leff + S = 2
Overall degeneracy for d1 (d2) case is 4 (5)
Multipolar spin exchange common for large Jeff
Multipolar interactions connect directly states with very different Sz quantum numbers  wavefunction delocalization in spin space

## Slide 20
Double perovskites
1.
A2BB′O6  regular ABO3 perovskites with alternating B (non-magnetic) and B′ (magnetic) atoms
Consequence of SOC  for Jeff = 3/2 the g-factor vanishes
Magnetic entropy (Rln(4)) estimated from experiments  indication of strong SOC
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.

## Slide 21
Multipolar exchange
2.
Consider Kugel-Khomskii type exchange with all orbitals are included  then project to the effective spins in the strong SOC limit
For d1 case consider exchange:
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.
Consider Kugel-Khomskii type exchange with all orbitals are included  then project to the effective spins in the strong SOC limit
In strong for t2g we have
Performing the projections we get
For d1 we have two exchange channels: ferromagnetic exchange between orthogonal orbitals (J′) and electrostatic quadrupole interaction (V)

## Slide 22
Mean field theory
3.
Exotic phases even in mean field
Anisotropic contributions come from quadrupolar and octupolar interactions
Antiferromagnetic phase for small J′/J and V/J
Ferromagnetic phases (FM110 and FM100) for large J′/J and V/J
Quadrupolar states classified by eigenstates of
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.
Only 1 independent eigenvalue (q, q, -2q)  Uniaxial nematic phase
2 independent eigenvalues (q1, q2, –q1, –q2)  Biaxial nematic phase
Quadrupolar phase appears in d2 perovskite even for T = 0; d1 must always break time reversal symmetry at T = 0 to avoid ground state degeneracy.

## Slide 23
Beyond mean-field theory
4.
Multipolar interactions destabilize conventional, magnetically ordered semiclassical ground states
More “spin flip” terms analogous to the Si+Sj– couplings
Quantum disordered ground states can be established rigorously for AKLT models
Multipolar Hamiltonians are intermediate between conventional spin models and these special cases
Check for disordered states  gauge the magnitude of quantum fluctuations within a spin-wave expansion
Valence bond solids and quantum spin liquid states predicted in various parameter regimes
Non-cubic crystal fields give highly frustrated systems  quantum fluctuations support a spin liquid phase
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.

## Slide 24
Connections to experiments
5.
Ba2YMoO6 cubic to low temperatures
Like many double perovskites has a two Curie regime
Phonon mode above 130 K; consistent with local structural change
Ba2NaOsO6 has a ferromagnetic ground state below 6.8 K with [110] easy axis
Landau theory predicts [100] or [111] as the easy axis
III. Strong Mott Regime
Partial degeneracy lifting and ordered double perovskites
B.
Quadrupolar ordering mechanism can account for it; associates with a structural change; not observed so far

## Slide 25
Not discussed  Ruddlesdon-Popper series of perovskite iridates  formula for a n-layer quasi-2D system  Srn+1IrnO3n+1 for n = 1, 2, ∞
The n = 1 case (Sr2IrO4) expected to be a high-Tc superconductor, upon doping, owing to its similarity cuprate parent compound to La2CuO4
This review mainly discusses bandwidth controlled MITs; filling (or doping) controlled MITs might reveal interesting physics
Exotic fractionalized phases possible: fractional Chern insulators from heterostructures of SrIrO3-SrTiO3
Controversies  Mott vs. Slater insulator in Sr2IrO4?  contradictory results from different calculations  experimental evidence needed
IV. Concluding Remarks and Outlook
Heterostructures of SrIrO3 and R2Ir2O7 along the [111] direction can give topological insulators and IQHE

## Slide 26
References
William Witczak-Krempa, Gang Chen, Yong Baek Kim, and Leon Balents. “Correlated quantum phenomena in the strong spin-orbit regime.” arXiv preprint arXiv:1305.2193 (2013)